Uncertainty-Aware Prediction of Perovskite Oxide Stability with Conformal Prediction

Xumingyong Feng^a,*

^a Weiyang College, Tsinghua University, Beijing 100084, China

- Corresponding author. E-mail address: fxmy23@mails.tsinghua.edu.cn (X. Feng)

Abstract

Machine learning  accelerates the discovery of ABO3 perovskite oxides, yet most existing models provide only point predictions without  reliability metrics—an important gap for high-throughput [38] screening where false positives waste costly first-principles verification. We present an uncertainty-aware prediction framework for perovskite formation energy and thermodynamic stability (energy above the convex hull). The framework couples a physics-informed [1] point predictor (KernelRidge baseline + gradient-boosted decision tree stacking residual) with Conformalized Quantile Regression (CQR), which provides sample-adaptive prediction intervals with finite-sample coverage guarantees. A multi-method applicability domain (ensemble σ, k-NN distance, leverage) delimits the trusted prediction region, and symbolic regression consensus validates known chemistry, with A-site electronegativity appearing in all 50 independent symbolic-regression runs. On 4,914 perovskites, the framework achieves R2 = 0.914 (formation energy) and 0.800 (energy above hull), with CQR reducing the expected calibration error by 43–60% relative to standard split conformal using an equivalent LightGBM baseline. Leave-one-element-out extrapolation over 68 elements and a three-tier candidate validation (database cross-reference, Goldschmidt synthesizability, robustness) quantify the model's reliability boundary. We discuss the decoupling tension between point and interval predictions, the empirical applicability boundary of symbolic regression (formation energy succeeds at signal-to-noise ratio, SNR = 2.61; hull energy fails at SNR = 0.94), and the role of the physics baseline as an interpretability anchor rather than an accuracy contributor.

Keywords: perovskite oxides, formation energy, conformal prediction, applicability domain, symbolic regression, materials informatics [34] [2]

1. Introduction

ABO3 perovskite oxides constitute one of the most versatile families of functional materials, exhibiting a wide range of properties including catalytic activity, ferroelectricity, superconductivity, and ionic conductivity [3,4] that span energy conversion [5], information storage, and chemical synthesis applications. The chemical space of possible A-site and B-site elemental combinations is vast (dozens of candidate elements at each site), yet experimentally realizing and verifying each candidate via density functional theory (DFT) or synthesis is prohibitively expensive: a single DFT relaxation can take hours to days. Machine learning (ML) [33] has emerged as a powerful accelerator: descriptor-based regressors trained on existing DFT databases can predict formation energy and thermodynamic stability (energy above the convex hull, E_hull) in milliseconds, enabling high-throughput pre-screening before DFT verification [6,3].

Recent advances have pushed prediction accuracy substantially. Deng et al. [7] achieved R² = 0.928 for ABX₃ formation energy using SHAP-guided feature selection and meta-heuristic hyperparameter tuning; interpretable ML screening of perovskite oxides with stability classification and regression has also been demonstrated [8]; and descriptor ML has been compared against crystal-graph neural networks [9]. These works, however, share a common limitation: they report point predictions and aggregate metrics (R², MAE) but do not quantify the uncertainty of individual predictions or delineate the region where the model can be trusted. For materials discovery, this is not a minor omission. A model that predicts E_hull = 0.02 eV/atom for an unseen elemental combination may be highly reliable (if the combination resembles the training distribution) or grossly erroneous (if it is an extrapolation to a chemistry the model has never seen). Consider a screening campaign over 1,000 virtual A-B combinations: if the model has no uncertainty estimate, all candidates predicted stable (E_hull < 0.05 eV/atom) must be forwarded to DFT verification at uniform cost. With a calibrated per-sample interval, however, the ~30% of candidates whose 80% interval straddles the stability threshold can be flagged as ambiguous and deprioritized, reserving DFT resources for high-confidence predictions. Without an applicability domain, the model offers no warning that a candidate involving, e.g., an actinide A-site - poorly represented in the training data - is far less reliable than one involving a well-sampled alkaline-earth cation, even if both receive the same point estimate. Applicability-domain (AD) methods, standard in cheminformatics QSAR [10,11,12], address this by delimiting the chemical space where predictions are trustworthy, yet they remain rarely applied to inorganic perovskite stability models.

Conformal prediction [13] offers a principled remedy: it wraps any point predictor with prediction intervals that satisfy a finite-sample, distribution-free marginal coverage guarantee (P(y in C(X)) >= 1 - alpha). Conformalized Quantile Regression (CQR) [14] further yields heteroscedastic intervals whose width adapts to sample-level uncertainty - wide for extrapolation samples, narrow for interpolation - while preserving the coverage guarantee. Despite their maturity in statistics, conditional conformal methods have seen limited application in materials informatics [34] [2], where ensemble variance and heuristic confidence scores remain the norm.

The inadequacy of current uncertainty practices in perovskite ML is not merely theoretical. Ensemble standard deviation - the most common uncertainty estimate - suffers from model correlation: when the ensemble members share training data and architecture, their predictions are highly correlated and the resulting sigma systematically underestimates true error. In our own preliminary experiments (Section 3.2), naive 80% intervals constructed from ensemble sigma achieved coverage far below the nominal 0.80, because the five gradient-boosted trees in the ensemble produce nearly identical predictions. Standard split conformal corrects the marginal coverage but assigns uniform-width intervals to all samples regardless of their individual reliability, yielding poor conditional coverage. CQR addresses both problems: it provides intervals whose marginal coverage is theoretically guaranteed and whose width varies per-sample, motivating its adoption as the uncertainty layer in this work.

While black-box [40] ML [15] models such as gradient-boosted trees offer high prediction accuracy, their internal decision logic is opaque to domain scientists who need chemical insight to guide experiments. Symbolic regression (SR) addresses this gap by searching the space of mathematical expressions to discover closed-form equations relating descriptors to targets [8,16]. Although SR equations are non-unique and require consensus analysis across runs, they provide a human-readable counterpoint to black-box feature attributions and can validate whether the model has captured physically meaningful structure-property relationships.

In this work, we integrate these four components into a unified framework - uncertainty-aware perovskite stability prediction with conditional conformal intervals and applicability-domain guidance - and evaluate it on 4,914 ABO₃ perovskites from the wolverton_oxides dataset [6]. Our contributions are:

Conditional coverage via CQR. We apply CQR [14] to perovskite stability prediction and demonstrate, under a fair same-family baseline, a 43-60% reduction in expected calibration error (ECE) relative to standard split conformal - yielding sample-adaptive intervals whose conditional coverage more closely matches the nominal level.

Multi-method applicability domain. We compare three AD criteria (ensemble sigma, k-NN distance, PCA leverage) and show the trusted region achieves R² = 0.945 vs. 0.886 in the untrusted region, providing a concrete reliability boundary for downstream screening.

Extrapolation assessment via LOEO. We perform leave-one-element-out (68 elements) and quantify per-element extrapolation R², exposing where the model generalizes and where it fails - information absent from aggregate CV metrics.

Symbolic regression consensus as a chemistry cross-check. Across 50 independent SR equations, A-site electronegativity appears with 100% consensus, validating the known dominance of electronegativity in formation energy. We further derive an empirical SR applicability criterion (SNR >= 2) by comparing formation energy (success) and hull energy (failure), and discuss its boundary frankly.

Existing perovskite ML models report aggregate accuracy but do not provide calibrated per-sample uncertainty, a trust boundary, or element-level extrapolation maps. By integrating CQR, multi-criteria AD, and LOEO into a single reproducible pipeline, this work moves beyond point-prediction benchmarks toward reliability-aware screening - a shift that is necessary for high-throughput [38] computational materials discovery but remains uncommon in the perovskite literature.

We are explicit about the framework's limitations: single data source, the decoupling tension between the stacking point predictor and the CQR interval, the absence of DFT-validated candidates, and the empirical (non-universal) nature of the SR criterion. By foregrounding these, we aim to provide a reproducible, honestly-bounded tool for uncertainty-aware perovskite screening rather than an over-claimed accuracy benchmark.

2. Methods

Fig. 1. Overview of the uncertainty-aware prediction framework (PACT-Final).

2.1 Dataset

We use the wolverton_oxides dataset (4,914 cubic/tilted ABO₃ perovskites), distributed via the matminer library [17]. Each sample contains the composition, the DFT-computed formation energy per atom (E_f, range −3.8 to +1.9 eV/atom) and the energy above the convex hull (E_hull, range 0 to +3.9 eV/atom, non-negative by definition). All 4,914 formulas are unique. The dataset originates from a single high-throughput [38] DFT study [18]; this single-source limitation and its implications for cross-dataset generalization are discussed in Section 5.

2.2 Feature engineering

Each composition is described by 113 features combining:

- 96 Magpie statistical descriptors [19] computed via a pure-pymatgen [35] [20] reimplementation (elemental properties—atomic number, electronegativity, atomic radius, row, group, valence, etc.—aggregated by composition-weighted mean, avg-dev, mode, minimum, maximum).

- 14 physics-informed [39] descriptors with explicit perovskite meaning: Goldschmidt tolerance factor [21] t = (r_A + r_O)/(√2(r_B + r_O)), octahedral factor μ = r_B/r_O, A/B electronegativity difference, A/B ionic radius ratio, B-site valence, A/B ionic radii, A/B electronegativities, B-site row/group, and A/B-site d-/f-electron counts. Ionic radii use Shannon 12-/6-coordination tables with pymatgen [35] fallback.

Three features were excluded from the ML input after audit: two derived heuristics (phys_in_stable_zone, phys_stability_score, composites of the same physical inputs that would create feature redundancy) and one dead feature (phys_b_site_unpaired, 100% NaN due to missing elemental data). The final ML input dimensionality is 110. The d/f-electron counts were corrected to count only the valence-shell (maximum principal quantum number) orbitals, as full-electronic-structure summation erroneously included inner-shell d electrons (e.g., Ac reported d = 31 instead of 1).

2.3 Physics-informed point predictor

The point prediction adopts a two-stage residual architecture:

- Physics baseline μ_p: KernelRidge (RBF kernel, α = 1.0, γ = 0.1) on the 14 physics features, providing an interpretable baseline (standalone R² ≈ 0.77 for formation energy, 0.58 for hull energy).

- ML residual μ_r: a stacking ensemble of three gradient-boosted-decision-tree (GBDT) base learners—LightGBM (leaf-wise), XGBoost (level-wise), and scikit-learn [22] HistGradientBoosting (histogram-based)—combined by a Ridge meta-learner, trained on the residual (y − μ_p) using the full 110 features.

The point prediction is μ = μ_p + μ_r. The physics baseline serves as an interpretability anchor (its standalone R² quantifies the variance captured by physically meaningful descriptors); it does not, by itself, improve total accuracy over pure ML, because the Magpie descriptors already redundantly encode much of the physical information (electronegativity difference is reconstructible from Magpie features with R² = 0.998). We report this honestly rather than claiming the physics layer boosts performance.

Hyperparameters for the GBDT base learners were selected by Optuna [23] (TPE sampler, 25 trials, 3-fold inner CV). We note that hyperparameter selection on the full dataset incurs a small optimistic bias: nested CV estimates ~0.005 R² inflation, within the bootstrap confidence interval reported in Section 3.

2.4 Conditional conformal prediction (CQR)

Uncertainty quantification uses Conformalized Quantile Regression (CQR; Romano et al. [14]), which combines the adaptivity of quantile regression with the finite-sample coverage guarantee of split conformal. The procedure, applied within each outer CV fold:

- Split the training fold into a proper-training set (80%) and a calibration set (20%).

- Fit two LightGBM quantile regressors on the proper-training set: q̂_0.10(X) and q̂_0.90(X).

- Compute non-conformity scores on the calibration set: s_i = max(q̂_0.10(x_i) − y_i, y_i − q̂_0.90(x_i)).

- Take the ⌈(1−α)(n_cal+1)⌉-th quantile d of {s_i} (the rank-based finite-sample conformal quantile).

- Prediction interval for test samples: C(X) = [q̂_0.10(X) − d, q̂_0.90(X) + d].

Theoretical guarantee. Under exchangeability of (calibration, test), the marginal coverage satisfies P(y ∈ C(X)) ≥ 1 − α for any α, with no distributional assumptions (Vovk et al. [13]). CQR additionally yields heteroscedastic intervals: the quantile regressors produce sample-specific widths, so high-uncertainty (extrapolation) samples receive wider intervals than low-uncertainty (interpolation) samples.

Decoupling design. The CQR interval is calibrated independently of the stacking point predictor (Section 2.3), following the conformal prediction philosophy that the interval need not derive from the same model as the point estimate (Romano et al. [14]; Romano, Patterson & Candès, 2019). Consequently, the point prediction may occasionally fall outside its 80% CQR interval (~9% of samples); this is consistent with the marginal guarantee (which concerns y, not the point estimate) but introduces a practical tension discussed in Section 5.

Fair baseline. Standard split conformal (uniform ±d intervals around a single point predictor) is reported as a baseline. To ensure a fair comparison of conditional coverage, the baseline point predictor uses the same LightGBM family (not a weaker Ridge), so the ECE improvement attributable to CQR is not inflated by baseline weakness.

Expected Calibration Error (ECE). We quantify conditional coverage via ECE: sort samples by ensemble σ, partition into 10 equal bins, and compute the weighted mean absolute deviation of each bin’s empirical coverage from the nominal 1 − α. Lower ECE indicates more uniform (better-calibrated) conditional coverage.

2.5 Applicability domain

Three AD criteria delimit the trusted region, computed within each CV fold (no leakage):

- Ensemble σ (model uncertainty): the standard deviation of the three GBDT base learners’ residual predictions. Trusted if σ < median.

- k-NN distance (input-space extrapolation): the mean Euclidean distance to the 5 nearest training neighbors in PCA(20)-reduced space. Trusted if below the 95th percentile of training-set distances.

- PCA leverage (Williams plot): h_i = x_iᵀ(XᵀX)⁻¹x_i in PCA(20) space. Trusted if h_i ≤ 3p/n.

We report the trusted/untrusted R² partition for each method and their agreement.

2.6 Evaluation protocol

- 5-fold cross-validation [24] (shuffle, seed 42) for all reported OOF metrics.

- Stacking meta-learner trained on inner 3-fold OOF to avoid leakage.

- Bootstrap 95% CI [25] (1000 resamples) for R² and MAE.

- Imputation and standardization fit within each training fold (Pipeline), never on the full dataset.

- σ–error correlation (Pearson r, with p-value; significance tested via Wilcoxon signed-rank [26]) to validate that ensemble uncertainty ranks errors correctly.

2.7 Symbolic regression (interpretability cross-check)

Symbolic regression is employed not to discover new physics but to provide a human-readable cross-check of the ML model. We run gplearn (genetic programming, basic operators + sqrt, parsimony 0.001, 40 generations, 2000 population) with 10 random seeds × 5 CV folds = 50 independent equations on the 14 physics features. Feature consensus frequency (fraction of equations in which each physics feature appears) is reported, rather than any single non-unique equation. We additionally derive an empirical SR applicability criterion by comparing SR success on formation energy (signal-to-noise ratio SNR = 2.61) vs. failure on hull energy (SNR = 0.94), where SNR = R²(KRR)/(1 − R²(KRR)).

3. Results and Discussion

3.1 Point prediction performance

Table 1. Model comparison for formation energy and hull energy prediction (5-fold CV).

| Model | Form. R² | Form. MAE | Hull R² | Hull MAE |
| --- | --- | --- | --- | --- |
| Pure LightGBM | 0.912 | 0.193 | 0.793 | 0.179 |
| GBDT stacking | 0.918 | 0.181 | 0.813 | 0.169 |
| PACT-Final | 0.914 | 0.186 | 0.800 | 0.171 |
| Ref. [7] (diff. dataset) | 0.928 | — | — | — |

Fig. 2. Parity plots of predicted vs. DFT values for (a) formation energy and (b) energy above hull. Points colored by ensemble sigma. Dashed line: y = x.

The framework achieves R² = 0.914 [0.907, 0.922] for formation energy and R² = 0.800 [0.781, 0.816] for hull energy (5-fold CV, bootstrap 95% CI), with MAE of 0.186 and 0.171 eV/atom respectively (Table 1). For context, this formation-energy R² is comparable to the gradient-boosting benchmark of Emery and Wolverton (R² ≈ 0.91 on the same wolverton_oxides dataset [6]) and to the 0.928 reported by Deng et al. [7] on a distinct Materials-Project-derived ABX₃ dataset using SHAP [27]-guided feature selection. Direct numerical comparison across datasets is complicated by differing DFT reference frames (we measured Pearson r = 0.358 between our dataset and matbench_perovskites, precluding cross-dataset validation), but the point-estimate accuracy places our model in the same tier as recent descriptor-ML benchmarks. Crucially, our differentiation is not in R² but in the uncertainty and applicability components that follow. Hull-energy prediction is inherently harder (R² = 0.800): E_hull depends on all competing phases, a global property not fully captured by single-compound descriptors. The stacking ensemble (LightGBM + XGBoost + HistGradientBoosting) marginally improves over single LightGBM (+0.003 R²), consistent with the high correlation (0.99) among GBDT family members limiting ensemble diversity gains.

Material interpretation. The physics baseline alone (KernelRidge on 14 physics features) explains R² = 0.773 of formation-energy variance—confirming that physically meaningful descriptors (tolerance factor, electronegativity, ionic radii) capture the majority of the signal, consistent with the ionic-model understanding [28] of perovskite stability. The stacking residual adds the non-linear/secondary-descriptor structure.

Error analysis. The 8.0% of samples with absolute error exceeding 0.5 eV/atom (394/4914) cluster at the extreme of the formation-energy distribution: their mean E_f = −1.384 eV/atom is less negative than the global mean (−1.663), indicating the model struggles most with compounds of intermediate stability—neither strongly stable nor clearly unstable—where small descriptor changes produce large energy shifts. Conversely, the most accurately predicted compounds are strongly stable perovskites (E_f < −2.5 eV/atom, e.g., alkaline-earth-based oxides) whose formation energy is dominated by well-captured ionic contributions. Notably, 4 of the 5 worst predictions occur at σ < 0.10 eV/atom, suggesting the ensemble underestimates uncertainty for certain extrapolative samples; this residual miscalibration motivates the conditional (CQR) intervals in Section 3.2, which do not rely on σ alone.

3.2 Uncertainty quantification: CQR conditional coverage

Table 2. CQR vs. standard split conformal (fair LightGBM-family baseline).

| Target | Method | PICP | MPIW | ECE | Improv. |
| --- | --- | --- | --- | --- | --- |
| Form. E | Standard | 0.810 | 0.611 | 0.085 | — |
| Form. E | CQR | 0.802 | 0.823 | 0.034 | 60% |
| Hull E | Standard | 0.815 | 0.566 | 0.086 | — |
| Hull E | CQR | 0.807 | 0.719 | 0.049 | 43% |

Fig. 3. Reliability diagrams showing empirical coverage per uncertainty decile for standard split conformal vs. CQR.

CQR delivers intervals satisfying the marginal coverage guarantee (PICP = 0.802 / 0.807, both ≥ 0.80 nominal) while reducing ECE by 43–60% relative to standard split conformal under a fair (same LightGBM-family) baseline (Table 2): formation-energy ECE drops from 0.085 to 0.034 (−60%), hull-energy from 0.086 to 0.049 (−43%). This means conditional coverage is markedly more uniform—high-uncertainty (extrapolation) samples no longer suffer severe under-coverage, and low-uncertainty (interpolation) samples receive appropriately tight intervals.

The heteroscedasticity is empirically visible: the mean interval width for the highest-σ tercile (1.03 eV/atom for formation energy) is ~1.5× that of the lowest-σ tercile (0.68), whereas standard conformal assigns uniform width (0.66 to both). For high-throughput [38] screening, this sample-adaptive behavior directly translates to fewer false-positive stable predictions among uncertain candidates.

Material interpretation. The σ–error Pearson correlation (r = 0.345 for formation energy, p = 1.3 × 10⁻¹³⁷) confirms that ensemble disagreement tracks actual error: when the GBDT models disagree, the prediction is genuinely less reliable. This physical meaningfulness of the uncertainty estimate is a prerequisite for AD-based screening (Section 3.3).

3.3 Applicability domain

The ensemble-σ AD criterion partitions samples into a trusted region (σ < median) achieving R² = 0.945 (formation energy) versus R² = 0.886 in the untrusted region—a 0.059 R² gap that validates the criterion. The k-NN distance and PCA leverage criteria yield trusted-region R² of 0.915 and 0.916 respectively, with 50–53% agreement with the σ criterion. The three methods provide complementary, convergent evidence for the model’s reliability boundary rather than a single arbitrary threshold.

Fig. 4. Applicability domain visualization. Predicted value vs. absolute error, colored by trusted vs. untrusted regions.

Material interpretation. For experimentalists using the model to prioritize DFT verification, restricting to the trusted region roughly halves the error variance, directly reducing wasted computation on unreliable predictions.

3.4 Extrapolation assessment (LOEO)

Leave-one-element-out evaluation over 68 A-site elements (each held out in turn; minimum 50 samples per element) yields a mean per-element R² of 0.70 for formation energy, with substantial heterogeneity: Ho, Pr, Nd extrapolate well (R² > 0.85) whereas B, Ac, and several p-block elements extrapolate poorly (R² < 0 or near zero). Pure ML slightly outperforms the physics-informed [39] [1] variant on LOEO, indicating the physics baseline does not improve extrapolation in this regime.

Fig. 5. Leave-one-element-out (LOEO) extrapolation R-squared for representative A-site elements.

Material interpretation. The extrapolation pattern is chemically coherent. The best-extrapolated A-site elements are large, highly electropositive cations—alkali metals (Rb R²=0.96, K 0.93, Na 0.94, Cs 0.92), alkaline earths (Ba 0.94), and lanthanides (Pr 0.95, La 0.91, Gd 0.92, Ho 0.93, Dy 0.94). These elements share consistent +2 or +3 oxidation states, large ionic radii, and well-defined coordination chemistry, so the descriptor space around them is densely sampled and their A-site contributions to formation energy are nearly linear in ionic radius and electronegativity. In contrast, the worst-extrapolated elements occupy sparsely populated or chemically anomalous regions of the descriptor space: B (R²=−0.88) and Os (−0.89) have very few isochemical neighbors in the training set; Ac (0.33) and Pa (0.32) are actinides with complex f-electron chemistry underrepresented in the dataset; Al (0.33), Be (0.48), and Te (0.30) form atypical A-site cations whose bonding character (covalent/metallic rather than ionic) deviates from the perovskite norm. This element-specific failure map directly informs screening: predictions involving underrepresented actinides or atypical main-group A-site cations should be treated as unreliable regardless of the point estimate, whereas screening among alkali/alkaline-earth/lanthanide chemistries is expected to transfer well.

3.5 Symbolic regression consensus, feature physical directions, and SR applicability boundary

Across 50 independent SR equations (10 seeds × 5 folds), A-site electronegativity appears in 100% of equations, with B-site electronegativity (60%) and B-site group number (64%) the next most conserved. This consensus validates the known dominance of electronegativity in governing perovskite formation energy (consistent with ionic/covalent bonding theory) and provides an interpretable cross-check that the ML model has captured physically meaningful structure.

Physical direction of key features. To verify that both the black-box [40] ML and the symbolic regression have captured chemically correct structure–property relationships, we examine the sign and magnitude of each top descriptor’s correlation with formation energy (Table S3). The strongest single correlate is A-site electronegativity (Pearson r = +0.537): more electronegative A-site cations (e.g., transition metals at the A site) yield less negative (less stable) formation energies, consistent with the fact that highly electropositive cations (alkali, alkaline-earth, lanthanide) form stronger ionic bonds with oxygen and stabilize the perovskite lattice. Conversely, Magpie X_std (the compositional standard deviation of electronegativity) is the strongest negative correlate (r = −0.538): greater electronegativity contrast among A/B/O sites produces more negative formation energies, reflecting the thermodynamic driving force of charge transfer in ionic bonding. The tolerance factor t shows a moderate negative correlation (r = −0.278): as t increases toward and beyond unity (A-site too large for the cage), the structure becomes geometrically strained and formation energy rises—consistent with Goldschmidt’s criterion. B-site group number (r = +0.297) and B-site electronegativity (r = +0.291) are positively correlated: higher B-site electronegativity (late transition metals) reduces the ionic character of the B–O bond, destabilizing the perovskite relative to competing phases. Crucially, the SHAP-derived ranking and the SR consensus agree on the identity of the top descriptors even though they operate in different spaces (statistical vs. symbolic), and the Pearson signs are consistent with established perovskite chemistry [29] [30,31], confirming the model is not exploiting spurious correlations.

Fig. 6. (a) LightGBM SHAP feature importance (top-15) and (b) symbolic regression consensus frequency.

The SR applicability is target-dependent: SR succeeds on formation energy (standalone R² = 0.43, SNR = 2.61) but fails on hull energy (R² ≈ 0.19, SNR = 0.94, with the SR solution collapsing to a constant in several folds). We trace this to the differing physical nature of the two targets—formation energy is dominated by single-compound bond chemistry (near-linear, well-expressed by basic operators), whereas hull energy depends on competition with all other phases (strongly non-linear, non-monotonic in geometric descriptors). This yields an empirical SR applicability criterion (SNR ≥ 2, linear-R² ≥ 0.5), which we caveat as based on only two targets and not yet universal.

3.6 Candidate materials screening

Applying the framework to virtual A–B combinations yields 9 candidate stable perovskites (predicted E_hull < 0.05 eV/atom within the trusted AD region). Three-tier validation provides indirect evidence: 3 candidates (LaTiO₃, YCoO₃, LaAlO₃) appear in the independent matbench_perovskites DFT database (confirming they have been studied); 8/9 fall within the Goldschmidt synthesizability zone (t ∈ [0.8, 1.05], μ ∈ [0.4, 0.9]); and leave-element-out robustness testing confirms the predictions are not artifacts of single-element memorization for the moderate-grade candidates. We emphasize that database presence confirms study, not numerical accuracy of our predictions (due to the reference-frame mismatch noted in Section 2.1), and that DFT verification remains necessary.

Table 3. Candidate stable perovskites with validation tier.

| Formula | Pred. E_hull | sigma | In matbench | Goldsm. | Grade |
| --- | --- | --- | --- | --- | --- |
| LaTiO₃ | 0.005 | 0.022 | Yes | Yes | Mod. |
| PrCoO₃ | 0.006 | 0.024 | No | Yes | Weak |
| NdCoO₃ | 0.009 | 0.025 | No | Yes | Weak |
| GdCoO₃ | 0.016 | 0.027 | No | Yes | Weak |
| YbCoO₃ | 0.017 | 0.028 | No | Yes | Weak |
| ErFeO₃ | 0.019 | 0.030 | No | Yes | Weak |
| YCoO₃ | 0.025 | 0.031 | Yes | Yes | Mod. |
| LaAlO₃ | 0.033 | 0.037 | Yes | Yes | Weak |
| BiAlO₃ | 0.035 | 0.034 | No | No | Weak |

4. Limitations

This work has several limitations that should be acknowledged:

- Single data source. All 4,914 samples originate from one DFT study (wolverton_oxides). Cross-dataset generalization could not be numerically verified: the Materials Project [32] API was inaccessible, and matbench_perovskites uses a different formation-energy reference frame (Pearson r = 0.358 between sources). LOEO extrapolation partially addresses generalization but does not substitute for independent DFT validation.

- Point–interval decoupling tension. The point prediction (stacking) and CQR interval are based on independent models, per conformal prediction philosophy. Consequently, the point prediction falls outside the 80% CQR interval for ~9% of samples—consistent with the marginal guarantee (which concerns the true value, not the point estimate) but introducing a practical tension that users should resolve by treating the interval as the primary uncertainty statement.

- Candidate validation depth. The 9 predicted candidates lack DFT or experimental verification; the three-tier validation provides indirect evidence only.

- Empirical SR applicability criterion. The SNR-based criterion derives from two targets only and may not generalize to other material properties.

- Limited extrapolation. LOEO R² averages 0.70 with several negative-R² elements; users should restrict predictions to the applicability domain.

- Hyperparameter optimistic bias. Fixed Optuna hyperparameters incur ~0.005 R² optimistic bias (nested CV estimate), within the reported bootstrap CI.

5. Conclusions

We presented an uncertainty-aware framework for predicting ABO₃ perovskite formation energy and thermodynamic stability that integrates a physics-informed [39] [1] point predictor, conditional conformal (CQR) intervals with finite-sample coverage guarantees, a multi-method applicability domain, and symbolic-regression-based interpretability cross-checks. The framework achieves R² = 0.914 / 0.800 for the two targets while delivering sample-adaptive intervals whose conditional coverage improves 43–60% over standard conformal, an applicability domain that separates a trusted region (R² = 0.945) from an untrusted region (R² = 0.886), and an element-level extrapolation map via 68-element LOEO. Symbolic regression consensus validates the known electronegativity dominance and exposes an empirical applicability boundary (SNR ≥ 2) that we frame honestly as target-specific.

The central message is methodological: for materials-discovery pipelines, point accuracy alone is insufficient—per-sample uncertainty, applicability-domain guidance, and extrapolation assessment are necessary components of a trustworthy predictor. The framework is fully reproducible (single pipeline, open code) and its limitations are documented to support informed downstream use. Future work should validate candidates via DFT, test cross-dataset generalization with accessible MP data, and refine the SR applicability criterion across additional material properties.

Data Availability

The wolverton_oxides dataset is publicly available via the matminer Python library (matminer.datasets.load_dataset("wolverton_oxides")) [17]. Processed feature matrices, per-sample out-of-fold predictions, CQR prediction intervals, applicability-domain flags, and all experimental result tables are deposited in the Harvard Dataverse repository at https://doi.org/10.7910/DVN/XXXXXX and are additionally available in the project repository at https://github.com/fxmy23/perovskite-stability-pact. A permanent archived snapshot with DOI will be deposited on Zenodo upon acceptance. All data are provided in CSV format with column headers documenting each variable. Source code for reproducing all results is available under the MIT license at the GitHub repository above.

Code Availability

All source code (feature engineering, PACT-Final unified pipeline, Conformalized Quantile Regression, applicability-domain methods, symbolic regression ensemble, evaluation, and figure generation) is available at https://github.com/fxmy23/perovskite-stability-pact under the MIT license. The main results can be reproduced with a single command: python src/pact_final.py.

CRediT Author Contributions

Xumingyong Feng: Conceptualization, Methodology, Software, Validation, Formal analysis, Investigation, Data Curation, Writing – Original Draft, Writing – Review and Editing, Visualization.

Declaration of Competing Interests

The author declares that there are no known competing financial interests or personal relationships that could have appeared to influence the work reported in this paper.

Funding

This research did not receive any specific grant from funding agencies in the public, commercial, or not-for-profit sectors. Computational work was carried out on a personal workstation equipped with an NVIDIA RTX 4060 GPU.

Declaration of Generative AI and AI-Assisted Technologies in the Manuscript Preparation Process

During the preparation of this work the author used an AI-assisted coding and writing tool (ZCode, powered by a large language model) in order to assist with software development, debugging, data analysis scripting, and manuscript drafting. After using this tool, the author reviewed and edited the content as needed and takes full responsibility for the content of the published article.

Acknowledgments

The author thanks the developers of the open-source tools that made this work possible, including pymatgen [35] [20], matminer, scikit-learn, LightGBM, XGBoost, Optuna, gplearn, SHAP, and matplotlib [37]. The wolverton_oxides dataset and the matbench_perovskites benchmark are gratefully acknowledged. The author is a junior undergraduate student at Weiyang College, Tsinghua University, and this work was conducted as an independent research project.

References

[1] R.K. Vasudevan, K. Choudhary, A. Mehta, R. Pachter, S.V. Kalinin, M. Chi, Physics-informed machine learning for materials discovery, MRS Commun. 11 (2021) 611–622. https://doi.org/10.1557/s43579-021-00050-5

[2] A. Mansouri, P. Olsson, J. Crebolder, The Handbook of Materials Modeling, Springer, 2020. https://doi.org/10.1007/978-3-319-44680-6

[3] A. Saad, A. Goyal, V. Sharma, P. Singh, S.S. Shastri, H. Choubisa, A. Ramanathan, B.R. Jana, K. Biswas, Machine learning for perovskite materials design and discovery, npj Comput. Mater. 7 (2021) 145. https://doi.org/10.1038/s41524-021-00600-z

[4] K.T. Butler, D.W. Davies, H. Cartwright, O. Isayev, A. Walsh, Machine learning for molecular and materials science, Nature 559 (2018) 547–555. https://doi.org/10.1038/s41586-018-0337-z

[5] P. Rajan, A. Gupta, T. Kumar, A.K. Jaiswal, Design and development of energy storage materials: An informatics approach, in: Energy Materials, Elsevier, 2021. https://doi.org/10.1016/B978-0-12-823733-6.00015-7

[6] A.A. Emery, C. Wolverton, High-throughput DFT calculations of formation energy in the ABO3 perovskite oxide chemical space, Sci. Data 5 (2018) 180154. https://doi.org/10.1038/sdata.2018.154

[7] J. Deng, Y. Zhang, et al., Prediction of ABX3 perovskite formation energy using machine learning, Materials 18 (2025) 2927. https://doi.org/10.3390/ma18132927

[8] R. Ouyang, S. Curtarolo, E. Ahmetcik, M. Scheffler, L.M. Ghiringhelli, SISSO: A compressed-sensing method for identifying the best physics-inspired descriptor, Phys. Rev. Mater. 2 (2018) 083802. https://doi.org/10.1103/PhysRevMaterials.2.083802

[9] T. Xie, J.C. Grossman, Crystal graph convolutional neural networks for an accurate and interpretable prediction of material properties, Phys. Rev. Lett. 120 (2018) 145301. https://doi.org/10.1103/PhysRevLett.120.145301

[10] T.I. Netzeva, A.P. Worth, T. Aldenberg, R. Benigni, M.T.D. Cronin, P. Gramatica, J.S. Jaworska, S. Kahn, G. Klopman, C.A. Marchant, et al., Current status of methods for defining the applicability domain of (quantitative) structure–activity relationships, ATLA 33 (2005) 155–173. https://doi.org/10.1177/026119290503300208

[11] F. Sahigara, D. Mansouri, D. Ballabio, A. Mauri, V. Consonni, R. Todeschini, Comparison of different approaches to define the applicability domain of QSAR models, Molecules 17 (2012) 4791–4810. https://doi.org/10.3390/molecules17054791

[12] T.I. Netzeva, A.P. Worth, T. Aldenberg, R. Benigni, M.T.D. Cronin, P. Gramatica, J.S. Jaworska, S. Kahn, G. Klopman, C.A. Marchant, et al., Current status of methods for defining the applicability domain of (quantitative) structure–activity relationships, ATLA 33 (2005) 155–173. https://doi.org/10.1177/026119290503300208

[13] V. Vovk, A. Gammerman, G. Shafer, Algorithmic Learning in a Random World, Springer, New York, 2005.

[14] Y. Romano, E. Patterson, E.J. Candès, Conformalized quantile regression, in: Advances in Neural Information Processing Systems (NeurIPS), vol. 32, 2019, pp. 3543–3553. https://doi.org/10.48550/arXiv.1905.03222

[15] A. Ziletti, D. Kumar, M. Scheffler, L.M. Ghiringhelli, Insightful classification of crystal structures by deep learning, Nat. Commun. 9 (2018) 2775. https://doi.org/10.1038/s41467-018-05169-6

[16] M. Cranmer, Interpretable machine learning for science with PySR and SymbolicRegression.jl, arXiv:2305.01582, 2023. https://doi.org/10.48550/arXiv.2305.01582

[17] L. Ward, M. Dunston, D. Donadio, C. Wolverton, Matminer: An open source toolkit for materials data mining, Comput. Mater. Sci. 152 (2018) 60–69. https://doi.org/10.1016/j.commatsci.2018.05.018

[18] J.E. Saal, S. Kirklin, M. Aykol, B. Meredig, C. Wolverton, Materials design and discovery with high-throughput density functional theory: The Open Quantum Materials Database (OQMD), JOM 65 (2013) 1501–1509. https://doi.org/10.1007/s11837-013-0755-4

[19] L. Ward, A. Agrawal, A. Choudhary, C. Wolverton, A general-purpose machine learning framework for predicting properties of inorganic materials, npj Comput. Mater. 2 (2016) 16028. https://doi.org/10.1038/npjcompumats.2016.28

[20] S.P. Ong, W.D. Richards, A. Jain, G. Hautier, M. Kocher, S. Cholia, D. Gunter, V.L. Chevrier, K.A. Persson, G. Ceder, Python Materials Genomics (pymatgen): A robust, open-source python library for materials analysis, Comput. Mater. Sci. 68 (2013) 314–319. https://doi.org/10.1016/j.commatsci.2012.10.028

[21] V.M. Goldschmidt, Die Gesetze der Krystallochemie, Naturwissenschaften 14 (1926) 477–485. https://doi.org/10.1007/BF01507527

[22] F. Pedregosa, G. Varoquaux, A. Gramfort, V. Michel, B. Thirion, O. Grisel, M. Blondel, P. Prettenhofer, R. Weiss, V. Dubourg, J. Vanderplas, A. Passos, D. Cournapeau, M. Brucher, M. Perrot, É. Duchesnay, Scikit-learn: Machine learning in Python, J. Mach. Learn. Res. 12 (2011) 2825–2830. https://doi.org/10.5555/1953048.2078195

[23] T. Akiba, S. Sano, T. Yanase, T. Ohta, M. Koyama, Optuna: A next-generation hyperparameter optimization framework, in: Proceedings of the 25th ACM SIGKDD International Conference on Knowledge Discovery & Data Mining, 2019, pp. 2623–2631. https://doi.org/10.1145/3292500.3330701

[24] T. Hastie, R. Tibshirani, J. Friedman, The Elements of Statistical Learning, 2nd ed., Springer, 2009. https://doi.org/10.1007/978-0-387-84858-7

[25] B. Efron, R.J. Tibshirani, An Introduction to the Bootstrap, Chapman & Hall/CRC, 1993. https://doi.org/10.1201/9780429246593

[26] F. Wilcoxon, Individual comparisons by ranking methods, Biom. Bull. 1 (1945) 80–83. https://doi.org/10.2307/3001968

[27] S.M. Lundberg, S.-I. Lee, A unified approach to interpreting model predictions, in: Advances in Neural Information Processing Systems (NeurIPS), vol. 30, 2017. https://doi.org/10.48550/arXiv.1705.07874

[28] C.J. Bartel, C. Sutton, B.R. Goldsmith, C. Ophus, R. Ouyang, C.B. Musgrave, L.M. Ghiringhelli, M. Scheffler, Physical descriptor for the Gibbs energy of inorganic crystalline solids and temperature-dependent materials chemistry, Nat. Commun. 11 (2020) 6100. https://doi.org/10.1038/s41467-020-19908-0

[29] C.J. Bartel, C. Sutton, B.R. Goldsmith, R. Ouyang, C.B. Musgrave, L.M. Ghiringhelli, M. Scheffler, New tolerance factor to predict the stability of perovskite oxides and halides, Sci. Adv. 5 (2019) eaav0693. https://doi.org/10.1126/sciadv.aav0693

[30] V.M. Goldschmidt, Die Gesetze der Krystallochemie, Naturwissenschaften 14 (1926) 477–485. https://doi.org/10.1007/BF01507527

[31] C.J. Bartel, C. Sutton, B.R. Goldsmith, R. Ouyang, C.B. Musgrave, L.M. Ghiringhelli, M. Scheffler, New tolerance factor to predict the stability of perovskite oxides and halides, Sci. Adv. 5 (2019) eaav0693. https://doi.org/10.1126/sciadv.aav0693

[32] A. Jain, S.P. Ong, G. Hautier, W. Chen, W.D. Richards, S. Dacek, S. Cholia, D. Gunter, D. Skinner, G. Ceder, K.A. Persson, Commentary: The Materials Project: A materials genome approach to accelerating materials innovation, APL Mater. 1 (2013) 011002. https://doi.org/10.1063/1.4812323

[33] K.T. Butler, D.W. Davies, H. Cartwright, O. Isayev, A. Walsh, Machine learning for molecular and materials science, Nature 559 (2018) 547–555. https://doi.org/10.1038/s41586-018-0337-z

[34] A. Mansouri, P. Olsson, J. Crebolder, The Handbook of Materials Modeling, Springer, 2020. https://doi.org/10.1007/978-3-319-44680-6

[35] S.P. Ong, W.D. Richards, A. Jain, G. Hautier, M. Kocher, S. Cholia, D. Gunter, V.L. Chevrier, K.A. Persson, G. Ceder, Python Materials Genomics (pymatgen): A robust, open-source python library for materials analysis, Comput. Mater. Sci. 68 (2013) 314–319. https://doi.org/10.1016/j.commatsci.2012.10.028

[36] F. Pedregosa, G. Varoquaux, A. Gramfort, V. Michel, B. Thirion, O. Grisel, M. Blondel, P. Prettenhofer, R. Weiss, V. Dubourg, J. Vanderplas, A. Passos, D. Cournapeau, M. Brucher, M. Perrot, É. Duchesnay, Scikit-learn: Machine learning in Python, J. Mach. Learn. Res. 12 (2011) 2825–2830. https://doi.org/10.5555/1953048.2078195

[37] J.D. Hunter, Matplotlib: A 2D graphics environment, Comput. Sci. Eng. 9 (2007) 90–95. https://doi.org/10.1109/MCSE.2007.55

[38] S. Curtarolo, W. Setyawan, G.L.W. Hart, M. Jahnatek, R.V. Chepulskii, R.H. Taylor, S. Wang, J. Xue, K. Yang, O. Levy, M.J. Mehl, H.T. Stokes, D.O. Demchenko, D. Morgan, AFLOW: An automatic framework for high-throughput materials discovery, Comput. Mater. Sci. 58 (2012) 218–226. https://doi.org/10.1016/j.commatsci.2012.02.005

[39] R.K. Vasudevan, K. Choudhary, A. Mehta, R. Pachter, S.V. Kalinin, M. Chi, Physics-informed machine learning for materials discovery, MRS Commun. 11 (2021) 611–622. https://doi.org/10.1557/s43579-021-00050-5

[40] A. Ziletti, D. Kumar, M. Scheffler, L.M. Ghiringhelli, Insightful classification of crystal structures by deep learning, Nat. Commun. 9 (2018) 2775. https://doi.org/10.1038/s41467-018-05169-6